หัวข้อวิจัย	อิทธิพลของโครงสร้างรูพรุนต่อสมบัติทางความร้อนของอิฐเซรามิกร่วมกับการเติมเศษวัสดุการเกษตร

ผู้ดำเนินการวิจัย	ผศ.ดร.อดิศักดิ์ ฦาชา และคณะ

หน่วยงาน	สาขาเทคโนโลยีอุตสาหกรรม (การผลิต) คณะวิศวกรรมศาสตร์

มหาวิทยาลัยราชภัฏมหาสารคาม

ปี พ.ศ.	2560

บทคัดย่อ

งานวิจัยนี้ศึกษาผลของการเติม เถ้าชานอ้อย ขี้เลื่อย และแกลบข้าวต่อสมบัติทางกายภาพ สมบัติเชิงกล และค่าการนำความร้อนของอิฐ นำมาผสมกับดินเหนียวในอัตราส่วนร้อยละ 0, 2.5, 5, 7.5 และ 10 โดยน้ำหนัก ตัวอย่างของอิฐทั้งหมดเผาที่อุณหภูมิ 900-1100 องศาเซลเซียส ผลการทดลองพบว่าค่าการหดตัวหลังการเผามีการหดตัวอยู่ระหว่าง 4 – 7 % ค่าการดูดซึมน้ำอยู่ระหว่าง 11 – 24 % ค่าความพรุนตัวอยู่ระหว่าง 20 – 40 % ค่าความหนาแน่นอยู่ระหว่าง 1.3 – 1.9 g/cm3 ค่าความแข็งแรงอยู่ระหว่าง 2.8 – 24 MPa และค่าการนำความร้องของอิฐใช้ขี้เลื่อย และแกลบข้าว เป็นส่วนผสมที่ 10 เปอร์เซ็นต์โดยน้ำหนักนั้น จะให้ค่าการนำความร้อนที่ต่ำคือ 0.16 W/mK และ 0.18 W/mK ในขณะที่อิฐที่ใช้เถ้าชานอ้อยเป็นส่วนผสม ค่าการนำความร้อนเท่ากับ 0.31 W/mK จากการเติมเถ้าชานอ้อยที่ 10 เปอร์เซ็นต์โดยน้ำหนัก ในขณะที่อิฐที่ไม่มีการเติมตัวเติมใดๆ พบว่าค่าการนำความร้อนอยู่ระหว่าง 0.84-0.96 W/mK

Research Title	Influence of porous structure on the thermal properties of ceramic 			brick with additive agricultural wastes

Researcher               Asst.Prof.Dr.Adisak Luecha and et al.

Organization             Industrial Technology (Manufacturing), Faculty of Engineering

Rajabhat Maha Sarakham University

Year                         2018

ABSTRACT

In this study, the effects of sugarcane bagasse ash, rice husk and sawdust additives on physical, mechanical and thermal conductivity of fired clay bricks were examined. Sugarcane bagasse ash, rice husk and sawdust incorporated to the clay body at the dosages of 0, 2.5, 5, 7.5 and 10 wt.%. All samples were fired at 900-1100 oC. The results indicated that the fired shrinkage was 4-7%, water absorption 11–24%, porosity 20–40%, bulk density 1.3–1.9 g/cm3, compressive strength 2.8–24 MPa, and thermal conductivity of fired clay bricks with 10 wt.% sawdust and rice husk was 0.16 and 0.18 W/mK, while bricks with 10 wt.% of sugarcane bagasse ash thermal conductivity was 0.31 W/mK. On the other hand, the control group, fired clay bricks without any wastes addition the values of thermal conductivity were 0.84-0.96 W/mK.